Datasheets for the mechanical properties of commercial Al alloys modified with micro-alloying technology

Table 1. Al-Si alloys

| Alloys | Casting process | Heat treatment condition(HTC) | Yield strength (YS, MPa) | Ultimate tensile strength (UTS, MPa) | Elongation (El, %) |
| --- | --- | --- | --- | --- | --- |
| A356 | Gravity casting | T61 | 180-240 | 250-290 | 3.0-6.0 |
| Modified A356 |  | T61 | 250-320 | 340-370 | 7.0-12.0 |

1T6: solutionising at 535±5°C for 6-8 hours with subsequently quenching into hot water of 60-80°C, then ageing at 165±5°C for 6-8 hours.

Table 2. Al-Cu alloys

| Alloys | Casting process | Heat treatment condition(HTC) | Yield strength (YS, MPa) | Ultimate tensile strength (UTS, MPa) | Elongation (El, %) |
| --- | --- | --- | --- | --- | --- |
| A206 | Gravity casting | T62 | 400-420 | 460-490 | 2.0-3.0 |
| Modified A206 |  | T62 | 460-510 | 520-540 | 3.0-6.0 |

2T6: solutionising at 525±5°C for 2-3 hours with subsequently quenching into hot water of 60-80°C, then ageing at 155±5°C for 8-10 hours.

Table 3. Al-Si-Cu alloys

| Alloys | Casting process | Heat treatment condition(HTC) | Yield strength (YS, MPa) | Ultimate tensile strength (UTS, MPa) | Elongation (El, %) |
| --- | --- | --- | --- | --- | --- |
| Mahle174 | Gravity casting | T63 | 190-260 | 200-280 | 0.5-1.0 |
| Modified Mahle174 |  | T63 | 250-320 | 320-380 | 0.5-1.0 |

3T6: solutionising at 510±5°C for 2-3 hours with subsequently quenching into hot water of 60-80°C, then ageing at 170±5°C for 8-10 hours.

Table 4. Al-Si-Mg alloys

| Alloys | Casting process | Heat treatment condition(HTC) | Yield strength (YS, MPa) | Ultimate tensile strength (UTS, MPa) | Elongation (El, %) |
| --- | --- | --- | --- | --- | --- |
| BD1 | High pressure die casting | T64 | 280-310 | 340-370 | 8.0-12.0 |
| Modified BD1 |  | T64 | 310-350 | 370-420 | 3.0-8.0 |

4T6: solutionising at 535 to 545±5°C for 30 min with subsequently quenching into hot water of 60-80°C, then ageing at 165 to 200±5°C for 6-8 hours.